## Slide 1: Molten Salt Energy Carrier Model Informed by the Pair Distribution Function
Jacob Numbers1, Anthony Birri2, Nick Termini2, Tyler Hamm1, Isaac Walker1, Troy Munro1
1Brigham Young University, Provo, UT
2Oak Ridge National Laboratories, Oak Ridge, TN

## Slide 2: Presentation Outline
Molten Salt Thermal Conductivity
Results
Previous Predictive Models
Model of Energy Carriers
Conclusion

## Slide 3: Foundational Challenges
[1] Nunes, V. M. B., M. J. V. Lourenço, F. J. V. Santos, M. L. S. M. Lopes, and C. A. Nieto de Castro. “Accurate Measurement of Physicochemical Properties on Ionic Liquids and Molten Salts.” In Molten Salts and Ionic Liquids, 229–63. John Wiley & Sons, Ltd, 2010. https://doi.org/10.1002/9780470947777.ch17
[2] Smith, A.L., 2022. Structure-property relationships in actinide containing molten salts – A review: Understanding and modelling the chemistry of nuclear fuel salts. Journal of Molecular Liquids 360, 119426. https://doi.org/10.1016/j.molliq.2022.119426
[3] Creasman, S., 2023. Sensitivity Analysis of Thermophysical Properties of Molten Salts using a Molten Salt Demonstration Reactor Model in TRANSFORM. Doctoral Dissertations.
[4] Magnusson, J., Memmott, M., Munro, T., 2020. Review of thermophysical property methods applied to fueled and un-fueled molten salts. Annals of Nuclear Energy 146, 107608. https://doi.org/10.1016/j.anucene.2020.107608
[5] Oak Ridge National Laboratory, U. of South Carolina, T. Besman, N. D. B. Ezell, T. Birri, N. Termini, S. Henderson, and J. Schorne-Pinto. (2024) Molten salt thermal properties database. [Online]. Available: https://mstdb.ornl.gov/
Molten Salt Thermal Conductivity (k)
Accurate reactor modeling
Optimized MSR design
Licensed MSRs
Competitive energy cost
Fundamental Physics
Predictive Models
Experimental Data
Data to validate connection between model and physics
Molten salt thermal conductivity needed to predict transient reactor behavior[1-3] and design safe MSRs
Accurate k measurements severely limited by high temperatures, corrosivity, and electrical conductivity of molten salts[4]
Predictive models can help fill in gaps in data, but require understanding fundamental physics for confident models

## Slide 4: Foundational Challenges
[1] Nunes, V. M. B., M. J. V. Lourenço, F. J. V. Santos, M. L. S. M. Lopes, and C. A. Nieto de Castro. “Accurate Measurement of Physicochemical Properties on Ionic Liquids and Molten Salts.” In Molten Salts and Ionic Liquids, 229–63. John Wiley & Sons, Ltd, 2010. https://doi.org/10.1002/9780470947777.ch17
[2] Smith, A.L., 2022. Structure-property relationships in actinide containing molten salts – A review: Understanding and modelling the chemistry of nuclear fuel salts. Journal of Molecular Liquids 360, 119426. https://doi.org/10.1016/j.molliq.2022.119426
[3] Creasman, S., 2023. Sensitivity Analysis of Thermophysical Properties of Molten Salts using a Molten Salt Demonstration Reactor Model in TRANSFORM. Doctoral Dissertations.
[4] Magnusson, J., Memmott, M., Munro, T., 2020. Review of thermophysical property methods applied to fueled and un-fueled molten salts. Annals of Nuclear Energy 146, 107608. https://doi.org/10.1016/j.anucene.2020.107608
[5] Oak Ridge National Laboratory, U. of South Carolina, T. Besman, N. D. B. Ezell, T. Birri, N. Termini, S. Henderson, and J. Schorne-Pinto. (2024) Molten salt thermal properties database. [Online]. Available: https://mstdb.ornl.gov/
Molten Salt Thermal Conductivity (k)
Thermal conductivity measurements of LiF and KCl4,5,6,7,8,24
See references page for plot citations
Chart: Avg. Estimated Uncertainty of Properties in MSTDB
| Density | Viscosity | Thermal Conductivity | Heat Capacity
Avg. Uncertainty (%) | 3.8 | 12.2 | 18.3 | 9.2
18%
12%
9%
4%
Chart: 
| 1st Qtr | 2nd Qtr
Sales | 5 | 26
Chart: 
| Thermal Conductivity Measurements | 2nd Qtr
Sales | 26 | 799
26 thermal conductivity measurements
5 actinide-bearing salts
820 salt compositions in MSTDB-TP[4]
Molten salt thermal conductivity needed to predict transient reactor behavior[1-3] and design safe MSRs
Accurate k measurements severely limited by high temperatures, corrosivity, and electrical conductivity of molten salts[4]
Predictive models can help fill in gaps in data, but require understanding fundamental physics for confident models

## Slide 5: Liquid Thermal Conductivity
Kinetic Theory of Gases
Dilute system – limited intermolecular interactions
Energy stored in individual molecules
Transferal rate via collisions proportional to molecular MFP
Energy Transfer in Liquids?
Phonon Physics of Solids
Significant interactions between molecules
Energy stored in vibrational modes in structure
Energy transferal rate proportional to excitation MFP
More like solids than gases:
Like solids, liquid energy carriers involve collective vibrations (phonon-like), diffusing atoms, electrons
Short-range ordering (SRO) evident in molten salts from pair distribution function (PDF) data
In molten salts, diffusion is limited at short time-scales[1] and only ions carry electric charge (limited free electrons), so vibrational excitations are dominant.
Challenges in modeling:
Lack of long-range order prevents conventional phonon description, and complex interactions limit dilute particle treatment.
[1] Turnbull, A.G., 1961. THE THERMAL CONDUCTIVITY OF MOLTEN SALTS. II. THEORY AND RESULTS FOR PURE SALTS. Australian J. Appl. Sci. Vol: 12.

## Slide 6: Previous Estimation Approaches
 | Liquid Theory |  |  |  |  | Fitting Methods
 | Phonon Gas Model (Zhao, 2021) (PGM) | Kinetic Theory (Gheribi) |  | Bridgman-type | Chapman-Enskog | Corresponding states, semi-empirical models
 |  | 2014 Empirical Fit (KTemp) | 2024 Kinetic Theory (KT24) |  |  | 
Energy Carriers | Phonon modes, approximated by macro-properties | Relates thermal conductivity to ionic radius proportionality by fitting to KCl data (Nagasaka, 1992) | Scales the Cahill-Poll minimum thermal conductivity according to anion complexity | Dilute gas interactions in a cubic lattice, relates λ to variation in free volumes/angles | Energy transfer occurs via collisions, modified with density and viscosity | Underlying thermal behavior follows across states of matter and certain materials
Temperature Dependence | Negative Based on temp-dependent sound velocity and density | Negative Based on thermal expansivity at melting point scaled with temperature change and composition |  | Negative Based on temp-dependent sound velocity and density | Negative Based on temp-dependent viscosity estimation | Matches temp-dependent behavior of fitted data
Limitations | Unknown phonon freq. distribution requires use of thermodynamic properties | Requires fitting to empirical data to scale the phonon mean free path relationship | Increased deviation with highly disparate ion mass (particularly actinides) | Does not consider dissociated interatomic behavior (prevalent in molten salt ions) | Does not capture the temperature dependence of salts. | May not be able to extrapolate for salt and compositional variation.
Molecular Interactions
Microscopic
Macroscopic
Thermodynamics
Dilute Gas
Solids
[1] Cahill, David G., S. K. Watson, and R. O. Pohl. “Lower Limit to the Thermal Conductivity of Disordered Crystals.” Physical Review B 46, no. 10 (September 1, 1992): 6131–40. https://doi.org/10.1103/PhysRevB.46.6131.
[2] Gheribi, A.E., A.T. Phan, and P. Chartrand. “A Theoretical Framework for Reliable Predictions of Thermal Conductivity of Multicomponent Molten Salt Mixtures: KCl-NaCl-MgCl2 as a Case Study.” Solar Energy Materials and Solar Cells 236 (2022). https://doi.org/10.1016/j.solmat.2021.111478.
[3] Gheribi, Aïmen E., and Patrice Chartrand. “Thermal Conductivity of Molten Salt Mixtures: Theoretical Model Supported by Equilibrium Molecular Dynamics Simulations.” The Journal of Chemical Physics 144, no. 8 (February 26, 2016): 084506. https://doi.org/10.1063/1.4942197.
[4] Gheribi, Aïmen E., Jesus A. Torres, and Patrice Chartrand. “Recommended Values for the Thermal Conductivity of Molten Salts between the Melting and Boiling Points.” Solar Energy Materials and Solar Cells 126 (July 1, 2014): 11–25. https://doi.org/10.1016/j.solmat.2014.03.028.
[5] Kincaid, John F., and Henry Eyring. “Free Volumes and Free Angle Ratios of Molecules in Liquids.” The Journal of Chemical Physics 6, no. 10 (October 1, 1938): 620–29. https://doi.org/10.1063/1.1750134.
[6] Nagasaka, Y., and A. Nagashima. “Corresponding States Correlation for the Thermal Conductivity of Molten Alkali Halides.” International Journal of Thermophysics 14, no. 4 (July 1, 1993): 923–36. https://doi.org/10.1007/BF00502115.
[7] Yang, Huiqiang, Ryan Gallagher, Patrice Chartrand, and Aïmen E. Gheribi. “Development of a Molten Salt Thermal Conductivity Model and Database for Advanced Energy Systems.” Solar Energy 256 (May 15, 2023): 158–78. https://doi.org/10.1016/j.solener.2023.04.009.
[8] Zhao, Andrew Z., Matthew C. Wingert, Renkun Chen, and Javier E. Garay. “Phonon Gas Model for Thermal Conductivity of Dense, Strongly Interacting Liquids.” Journal of Applied Physics 129, no. 23 (June 21, 2021). https://doi.org/10.1063/5.0040734.

## Slide 7: Previous Model Analysis
Models typically describe thermal conductivity in terms of a scale factor of energy storage, group velocity, and MFP of energy carriers
Model performance relative to measurements can help reveal physical mechanisms governing molten salt thermal conductivity
Gheribi Kinetic Theory, Cahill-Poll λmin (KTCPλ):
Zhao Phonon Gas Model (PGM):
Bridgeman-type:
Temp-varying modifier
Adjust to accounts for rotational, vibrational DOF
Normalized net flux in 1 of 3 dimensions
Adjusts MFP for valency

## Slide 8: Previous Model Analysis
Strengths
Assumes bulk volumetric properties approximate phonon characteristics per unit volume, conceptually links measured cp and vs to energy carriers.
Weaknesses
Assumes that mean free path is approximated by average interatomic distance—causes underestimations of nearly all salts
See references page for plot citations
Strengths
Temp-dependent adjustment based on thermodynamic link between thermal expansivity and k.
Latest iteration of Gheribi’s kinetic theory accounts for damping to conductivity caused by complexes
Weaknesses
Large ion mass disparity causes significant error due to mass fluctuation term in the case of actinides.
  Complexation factor further reduces k for actinide-bearing salts
Gheribi – Kinetic Theory
Zhao – Phonon Gas Model
Other Models
Perform poorly for complex, strongly-interacting, binary liquids
Case study comparisons help clarify correct physical mechanism in various formalisms.
Notes: KT currently the most successful model

## Slide 9: Modeling Actinides
Gheribi - Kinetic Theory
KT methods build compositional dependency using a modifier to ideal conductivity, with a factor of mass fluctuation
KT performs well with ions of similar molar masses, but degrades with increasing disparity of molar mass, providing unrealistic estimations for actinides
MUF4 = 314 g/mol
MLiF = 25.9 g/mol
FLiBe+2%UF4
FLiBe
PGM underpredicts most λ, but approaches measured value with increased actinide presence. Why?
What we need:
More actinide data with compositional/temperature variation
Develop modeling ability for actinides
Reference 31

## Slide 10: Model Performance
Does the variation in model results sufficiently replicate measurement uncertainty?
KT uses fundamental mixing rules for property values (Cp, Vm, vsound)(cite Gallagher). These are applied to PGM for analysis.
Mm and vsound dominant influential parameters in both Gheribi and Zhao models; molten salt sound velocity values are subject to significant uncertainty.
Gheribi’s Cahill-Poll λmin provides best parameter sensitivity confinement
 | KTemp |  | KTCP | PGM
vsound,m | 15% |  |  | -2.1%
v’sound (slope) |  |  |  | 21%
Vm | -15% |  |  | -1.3%
V’ (slope) |  |  |  | 14%
Cp | 15% |  |  | 15%
%Deviation of estimated properties using mixing rules from measured values for eutectic FLiNaK
Comparison of FLiNaK model predictions using mixture values obtained via measurements or fundamental mixing rules.
See reference 10

## Slide 11: New PDF-informed Thermal Conductivity Model

## Slide 12: Energy Carriers in a Coherent Medium
Simplifying the Liquid Approach
[1] Landau, Lev Davidovich, and Evgeny Mikhailovich Lifshitz. Course of Theoretical Physics. Vol. 5, Statistical Physics, Part 1. Pergamon Press, 1970.
Monatomic, dilute gas
1. Heat is transferred by some dominant form of energy carrier(s)
2. These propagate with effective properties while coherent medium
Two general principles
Electrons
Atoms
Photons
Phonons
Transparent Solid
Metal
Empty space
Perfect crystal
x=0
Hot
Cold
x
y
z
x-λ
x+λ
Mean free path before collision (energy transfer)
Once medium coherence ends (crystal defect, collision between atoms, etc.) the energy carrier transfers its energy to new carrier
The spatial and temporal extent of coherence determines mean free path
The properties of any interacting system are governed by its excitations—the energy carriers[1].

## Slide 13: Review - Kinetic Theory
Generalized Energy Carriers
Kinetic theory model works for ideal gases because there exists only one type of energy carrier with measurable average attributes (number density, velocity, volumetric heat capacity).
For generalized energy carriers, the problem becomes how to characterize and measure energy carriers.
Unit volume in terms of average velocity
dx
dA
Unit area
Unit distance
Number density
Unit distance travelled in unit time 𝑑𝑡 at average velocity ⟨𝑣⟩
Number of energy carriers (particles, phonons, etc.) that will cross plane of unit area per unit time
+x
-x
1/6 will be moving towards surface
x
y
z
1/3 of particles will have motion in any given direction
x
y
z

## Slide 14: Review - Kinetic Theory
Generalized Energy Carriers
To define , we need to characterize the effective heat capacity, group velocity, and mean free path of the energy carriers.
x=0
Hot
Cold
x
y
z
x-λ
x+λ
Mean free path before collision (energy transfer)
Change in energy across unit plane per unit time—heat flux
Energy change proportional to definition of internal energy
Taylor series of about
Thermal conductivity in terms of energy carrier properties
Volumetric constant pressure specific heat capacity
Heat flux in terms temperature gradient

## Slide 15: Energy Carriers in a Coherent Medium
Kinetic Theory of Gases
For a monatomic gas, only 1 dominant energy carriers (atoms) with characteristic:
Heat capacity/particle particle kinetic energy ()
Velocity (avg of Maxwellian distribution)
Mean free path between collisions
The heat flux is the energy crossing a hot-cold gradient surface:
Thermal conductivity in terms of energy carrier properties
Heat flux in terms temperature gradient
Monatomic, dilute gas
x=0
Hot
Cold
x
y
z
x-λ
x+λ
Mean free path before collision (energy transfer)

## Slide 16: Energy Carriers in a Coherent Medium
Analogy to General Energy Carriers
[1] Trachenko, K., 2023. Theory of Liquids: From Excitations to Thermodynamics. Cambridge University Press, Cambridge. https://doi.org/10.1017/9781009355483
[2] Frenkel, J., 1946. Kinetic theory of liquids, International series of monographs on physics. Clarendon Press, Oxford.
If we can characterize the dominant energy carriers over range of liquid state, we could calculate .
1 longitudinal phonon mode
2 transverse phonon modes (generally negligible in liquids, high Frenkel frequency)[2]
Exactly what the phonon thermal conductivity model describes — integrates properties across phonon frequencies.
But in liquids, there is a variable phase space[1], i.e. as temperature increases, viscosity/diffusion limit phonon wavelengths
Increasing temperature

## Slide 17: Properties—Macro to Micro
Characterizing Energy Carriers
Assuming effective properties of energy carriers, neglecting transverse modes
1 longitudinal phonon mode
2 transverse phonon modes (generally negligible in liquids, high Frenkel frequency)
 | Specific Heat Capacity – | Group Velocity – | Mean Free Path -
Metric | Measured bulk volumetric specific heat | Measured adiabatic speed of sound | Structural coherence length
Reasoning | Successful heat capacity model links phonon states to liquid characteristics[1]. | The macroscopic limit of longitudinal modes give rise to the adiabatic sound velocity[4] | Short-range vibrational modes are dominant energy transfer medium[7]—the average structural coherence length is proportional to short-range order
Questions | Low velocity modes contribute to heat capacity but not thermal conductivity[2]—provides an upper bound[3]. | Molten salts do support shear modes and faster group velocities at very small wavelengths corresponding to interatomic distances[5,6], but dampen quickly and not dominant[3]. | How do we obtain the effective structural coherence length? How is the coherence of energy transfer affected by structure and liquid diffusion?
 | Populations of transverse modes appear to be very small in proportion to longitudinal modes; these may be considered negligible[4] |  | 
Metric | Measured bulk volumetric specific heat | Measured adiabatic speed of sound | Structural coherence length
Reasoning | Successful heat capacity model links phonon states to liquid characteristics[1]. | The macroscopic limit of longitudinal modes give rise to the adiabatic sound velocity[4] | Short-range vibrational modes are dominant energy transfer medium[7]—the average structural coherence length is proportional to short-range order
Questions | Low velocity modes contribute to heat capacity but not thermal conductivity[2]—provides an upper bound[3]. | Molten salts do support shear modes and faster group velocities at very small wavelengths corresponding to interatomic distances[5,6], but dampen quickly and not dominant[3]. | How do we obtain the effective structural coherence length? How is the coherence of energy transfer affected by structure and liquid diffusion?
 | Populations of transverse modes appear to be very small in proportion to longitudinal modes; these may be considered negligible[4] |  | 
What temperature and composition-dependent, measurable parameters characterize the dominant energy carriers?
[1] K. Trachenko, “Heat capacity of liquids: An approach from the solid phase,” Phys. Rev. B, vol. 78, no. 10, p. 104201, Sep. 2008, doi: 10.1103/PhysRevB.78.104201.
[2] D. G. Cahill, S. K. Watson, and R. O. Pohl, “Lower limit to the thermal conductivity of disordered crystals,” Phys. Rev. B, vol. 46, no. 10, pp. 6131–6140, Sep. 1992, doi: 10.1103/PhysRevB.46.6131.
[3] Chen, G., 2005. Nanoscale Energy Transport and Conversion: A Parallel Treatment of Electrons, Molecules, Phonons, and Photons. Oxford University Press.
[4] A. Z. Zhao, M. C. Wingert, R. Chen, and J. E. Garay, “Phonon gas model for thermal conductivity of dense, strongly interacting liquids,” Journal of Applied Physics, vol. 129, no. 23, Jun. 2021, doi: 10.1063/5.0040734.
[5] K. Trachenko, Theory of Liquids: From Excitations to Thermodynamics. Cambridge: Cambridge University Press, 2023. doi: 10.1017/9781009355483.
[6] F. Demmel, S. Hosokawa, and W. C. Pilgrim, “Collective particle motions in molten KCl,” Journal of Alloys and Compounds, vol. 452, no. 1, pp. 143–148, Mar. 2008, doi: 10.1016/j.jallcom.2006.10.167.
[7] K. Cornwell, “The thermal conductivity of molten salts,” J. Phys. D: Appl. Phys., vol. 4, no. 3, p. 441, Mar. 1971, doi: 10.1088/0022-3727/4/3/313.

## Slide 18: Pair Distribution Function
Short Range Liquid Structure
The pair distribution function (PDF) gives the probability distribution of interatomic spacing—can be obtained from X-ray and neutron diffraction experiments.
The partial PDF gives the probabilities of separation distances for individual ion pairs—this is most often done using AIMD simulations and then validating with the total experimental PDF
Normalized by radial distance, the partial PDF provides the probability gAB(r) of finding an ion B a distance r from reference ion A.
Can the PDF provide information about the mean free path of energy carriers?
[1] Smith, A.L., 2022. Structure-property relationships in actinide containing molten salts – A review: Understanding and modelling the chemistry of nuclear fuel salts. Journal of Molecular Liquids 360, 119426. https://doi.org/10.1016/j.molliq.2022.119426
[2] Frandsen, B.A., Nickerson, S.D., Clark, A.D., Solano, A., Baral, R., Williams, J., Neuefeind, J., Memmott, M., 2020. The structure of molten FLiNaK. Journal of Nuclear Materials 537, 152219. https://doi.org/10.1016/j.jnucmat.2020.152219
(a) Experimental PDF and (b) modeled partial PDF of molten FLiNaK.
B. A. Frandsen et al. Journal of Nuclear Materials (2020)[2]
g(r)
r
1
Gas
r
g(r)
1
Solid Crystal
r
g(r)
1
Liquid
Liquids lack long-range periodicity of crystal, but have preferential arrangements at short distances.

## Slide 19: Structural Coherence Length
Interpreting the Pair Distribution Function
Assumptions:
Cation-anion pairs are dominant medium in energy transfer (strongest bonds, charge-ordering).
Energy carriers (phonons, sequential ion collisions, etc.) will propagate as long as its medium remains coherent.
Structural coherence length is proportional the degree of short-range order in molten salts.
Chart: 
| 2.662654071 | 6.0470420550000004 | 9.7622348789999993 | 13.299302020000001
 | 1.0719 | 0.11862 | 0.034873 | 0.014759
Concentration of ion pair
Thermal energy transferred
Energy must be redistributed wherever structural coherence ends
Some portion continues to the extent of a coherent medium
Bulk number density
What information from the PDF informs ?
Perfect decay function fitting indicates that mechanisms for coherence decay in first coordination shell continue with r.
How does coherence change with distance?

## Slide 20: Structural Coherence Length
Interpreting the Pair Distribution Function
Chart: 
| 2.662654071 | 6.0470420550000004 | 9.7622348789999993 | 13.299302020000001
 | 1.0719 | 0.11862 | 0.034873 | 0.014759
Concentration of ion pair
Thermal energy transferred
Energy must be redistributed wherever structural coherence ends
Some portion continues to the extent of a coherent medium
Bulk number density
What information from the PDF informs ?
How does coherence change with distance?
Rules for coherency:
The ideal recipients of energy carriers are oppositely charged ions separated by distance of interaction potential minima (most efficient transfer)
Decoherence results in the transfer of energy to system—new energy carriers
Interacting with a non-ideal recipient breaks coherence. Non-ideal recipients include:
  Same-charge ions
  Dissimilar next-ions from the originating ion
  Out-of-phase transfer

## Slide 21: Structural Coherence Length
Coherence Survival Function
If energy carriers are emitted from an energized cation over time, the surviving carriers will decrease by over a distance according to the probability of transferring energy to non-ideal recipients—the disruption probability function .
The change in the number of energy carriers according to over distance
Rearranging and solving for the number of energy carriers as a function of radius
The fraction of energy carriers remaining at a distance
Cumulative survival probability function

## Slide 22: Structural Coherence Length
Coherence Survival Function
Area under normalized cumulative survival function is the average distance of energy transfer—the average structural coherence length
If can be accurately approximated, the average structural coherence length can be calculated
r
g(r)
1
r
S(r)
1
Liquid

## Slide 23: Structural Coherence Length
Scaling Contributions to Decoherence
If multiple relative decoherence factors are present, then the sum of their expressions for allow each to either cause or have no effect
is equal to when , or when
 | All carriers stop at r | No carriers stop at r
 | -S | 0
 |  | 0
 | 1 | 0
 | All carriers stop at r | No carriers stop at r
 | -S | 0
 |  | 0
 | 1 | 0
To not require an absolute value for decoherent factors ranging from 0 to ∞, we can define relative decoherence factors as a ratio between 0 and 1, which either cause or for each limit.
r
1

## Slide 24: Structural Coherence Length
Disruption Function
Most efficient separation distance for vibrational energy transfer. The first peak corresponds to the energy minima, so any other transfer position is assumed decoherent
Disruption factors :
Calculated at discrete transfer radii because the ideal coherent medium is a sequential chain of cation-anion-cation-anion-etc. Assumes other interaction distances leads to decoherence.
The interval spacing for efficient transfer are given by the first peak distance for each cation-anion pair, corresponding to the energy minima[1].
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
Subsequent peaks are not determined by interaction potential with central ion—dictated by packing density

## Slide 25: Structural Coherence Length
Disruption Function
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
Most efficient separation distance for vibrational energy transfer.
Disruption factors :
: Non-ideal recipient probability factor
Chances of interacting with a like-charge ion instead of ideal oppositely charged ion (typically very small due to charge ordering).
Dependent only on the first peak, which is gives the probability distribution around any ion in the chain.
Accounts for the potential decoherence caused by non-deal recipient ions
Applied starting at second transfer

## Slide 26: Structural Coherence Length
Disruption Function
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
High ratio of peak height to first minima corresponds to very strong bond
Subsequent peaks are not determined by interaction potential with central ion—dictated by packing density
Non-zero first minima indicates relative affinity for diffusion
Disruption factors :
: Non-ideal recipient probability factor
: Bond strength factor
Ratio between 0 (bond allows no ions to escape) and 1 (no interaction between ions), related to diffusion coefficient[1].
This accounts for the potential inefficiency of energy transfer across a cation-anion pair
Applied starting at second transfer
[1] Hines, A.L., Walls, H.A., 1979. Determination of self diffusion coefficients using the radial distribution function. Metall Trans A 10, 1365–1370. https://doi.org/10.1007/BF02811992

## Slide 27: Structural Coherence Length
Disruption Function
Disruption factors :
: Non-ideal recipient probability factor
: Bond strength factor
: Phonon transfer factor
Ratio of encountering ion other than given ion pair.
This accounts for the potential inability of an ion chain to sustain a phonon—requires at least 3 ions
Applied starting at third transfer
Relative bond strength given by peak-minima ration, exponent simulating the Leonard-Jones potential attractive term
For
Assuming out-of-phase phonons cannot be sustained
Harmonic oscillator frequency function of bond strength and reduced mass
Reduced mass of cation-anion pair
Relative proportional frequency factor
Decoherence induced proportional to concentration of ion pair

## Slide 28: Structural Coherence Length
Disruption Function
Disruption factors :
: Non-ideal recipient probability factor
: Bond strength factor
: Phonon transfer factor
Ratio of encountering ion other than given ion pair.
This accounts for the potential inability of an ion chain to sustain a phonon—requires at least 3 ions
Applied starting at third transfer
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
+
+
-
+
+
-
Dissimilar ions cannot sustain minimum vibrational mode; transfer ends at first ion
Ion sequence of similar masses/bond strength can sustain coherent longitudinal wave

## Slide 29: Structural Coherence Length
Chart: 
| 0.32173865816239788 | 0 | 0
+- Peaks
++ Peaks
1.561460361 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
1.965824666 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452 | 0
Chart: 
| 0.32173865816239788 | 0 | 0
+- Peaks
++ Peaks
1.561460361 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
1.965824666 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452 | 0
Disruption Function
Disruption factors :
: Non-ideal recipient probability factor
: Bond strength factor
: Phonon transfer factor
Energy will travel at least the first bond distance—whether it continues past this point depends on the probability of coherency
The factors account for probability of decoherent events at each transfer distance
+
+
-
+
+
-
+
-

## Slide 30: Structural Coherence Length
Disruption Function
Summary:
Ideal coherence starts at an infinite chain of cation-anion-etc.
Perturbations from ideality drop the structural coherence length according to probabilities of non-coherence factors
The minimum path length is the transfer distance between the first cation-anion pair.
  ↑Why the effect of Umklapp scattering, 4-phonon scattering reaches max effect—no T3 temperature dependence.
Further development will weight specific heat, speed of sound to estimate each ion pair’s relative contributions

## Slide 31: Results
Compared to Back-Calculated
Analysis:
13 alkali/alkaline-earth halide salts were analyzed using experimental k and MD simulation PDF data from various literature sources.
Back-calculated structural coherence length provided initial comparisons to present model predictions
Further development will weight specific heat, speed of sound to estimate each ion pair’s relative contributions

## Slide 32
Chart: SCL_Calc
| 1.2767938196406401 | 0.75631548066380605 | 0.497568288937763 | 0.77860022830973397
#REF! | 1.1 | 0.78633 | 0.76698 | 0.86545
#REF! | 1
Ideal | 0 | 2
Chart: kpredicted
| 1.27254998016219 | 0.85709429236785095 | 0.571754421134825
Unary Flourides | 1.2682 | 1.2193 | 0.62201
Unary Chlorides | 0.62172 | 0.47705 | 0.3656
Unary Alkaline Earth Chlorides | 0.79108
Fluoride Mixtures | 1.1 | 0.78633
Chloride Actinide Mixtures | 0.23926 | 0.27567
Water | 0.561
Ideal | 0 | 2
Comparison to Experimental Data
The present general energy carriers model performs well for range of salts.
Some discrepancy for divalent alkaline earth halide salts, but measurement data is limited.
Results
Comparison of measured thermal conductivity to the present model

## Slide 33
The present model performs comparably well with Gheribi’s kinetic theory for unary and mixture salts
“Mix Data” indicates models used the same measured values for speed of sound, specific heat, and density of the mixture
When no mixture data was available, the models used fundamental mixing rules for cp, v, and density of the mixture.
Results
Model Comparison

## Slide 34: Results
Chart: kpredicted
| 1.3498414938304 | 0.842268101058265 | 0.58268227937308503 | 0.68631947375037605 | 0.48682954154178998 | 0.37423569928907002 | 0.43829220310135403 | 0.448735993317051 | 0.383511707903748
Kinetic Theory - Unary Salts | 1.2682 | 1.2193 | 0.62201 | 0.62172 | 0.47705 | 0.3656 | 0.79108
Kinetic Theory - Mixtures | 1.1 | 0.78633 | 0.76698 | 0.86545
Kinetic Theory - Actinides | 0.23926 | 0.27567
Present Model - Unary Salts | 1.2682 | 1.2193 | 0.62201 | 0.62172 | 0.47705 | 0.3656 | 0.79108
Present Model - Mixtures | 1.1 | 0.78633 | 0.76698 | 0.86545
Present Model - Actinides | 0.23926 | 0.27567
Ideal | 0 | 2
115% | 1.4585 | 1.4022 | 0.71531 | 0.71497 | 0.54861 | 0.42044 | 0.90974 | 1.265 | 0.90428 | 0.88203 | 0.99527 | 0.27515 | 0.31703
0.85 | 1.078 | 1.0364 | 0.52871 | 0.52846 | 0.4055 | 0.31076 | 0.67242 | 0.935 | 0.66838 | 0.65194 | 0.73563 | 0.20337 | 0.23432
Model Comparison
Present model better approximates actinide-bearing salt measurement data than kinetic theory.
Results support possible connection between bulk thermophysical properties and energy carrier properties
-15%
+15%

## Slide 35: Conclusions
Successes
Present model makes direct connection between molten salt structure and MFP using the PDF
Quantifies disruption factors relative to absolute limits, with no adjustable terms
In preliminary analysis, predictions approximate measured values for both unary salts and mixtures, including actinides
Limitations
Requires partial PDF of the mixture to predict thermal conductivity
Disruption factors may have nonlinear effects
Limited by accuracy of PDF and mixing rules for specific heat and sound velocity
State of the Model

## Slide 36: Outlook
Further Development to Implement
Because each cation-anion pair i contribute variably to cp and vs, the total thermal conductivity should be a weighted sum of each pair’s effective contribution.
Weighting these contributions should increase prediction accuracy
Data Needed
Only a limited number of salts were analyzed; more rigorous development will need:
PDFs for all halide unary salts, particularly unary actinide salts
PDFs for key actinide mixtures
Thermal conductivity measurements for more actinide bearing salt mixtures
  Compositional studies around the eutectic point will point to trends between composition and k
State of the Model

## Slide 37
Summary
Understanding physical mechanisms underlying molten salt thermal conductivity will enable increased predictability and MSR optimization
Linking liquid structure to thermophysical properties can provide insights for liquid molecular energy transport theory
Actinide-bearing salts have been successfully predicted, but more experimental and PDF data is needed to validate full extent of model
Future Work
Upcoming k measurements at BYU of various compositions of NaCl-UCl3 with respective partial PDFs to observe compositional
Potential to generalize model using endmember PDFs (instead of full mixture) to provide full predictive thermal conductivity model for actinide-bearing salts

## Slide 38: Acknowledgements
Funding for this research has come from the Department of Energy, Nuclear Energy University Program (NEUP): Award #DE-NE0009502.
Anthony Birri and Nicholas Termini are supported by the Molten Salt Reactor Program and the Nuclear Energy Advanced Modeling and Simulation Program under the US Department of Energy’s Office of Nuclear Energy.
Meaningful discussions with Benjamin Frandsen and Matthew Asplund also provided valuable direction for the project. The authors are also grateful for the assistance of Tyler Hamm, Britton Baltich, Isaac Cutler, and Lizzy Robinson in compiling and interpreting data for this work.
Presentation slides

## Slide 39
References for Plot Data
M.-M. Walz and D. van der Spoel. “Molten Alkali Halides: Temperature Dependence of Structure, Dynamics and Thermodynamics.” Physical Chemistry Chemical Physics 21, no. 31 (2019): 17252–17264.
R. L. McGreevy. “Experimental Studies of the Structure and Dynamics of Molten Alkali and Alkaline Earth Halides.” In Solid State Physics, edited by H. Ehrenreich and D. Turnbull, vol. 40, 247–325. New York: Academic Press, 1987.
S. Tahara, H. Toyama, H. Shimakura, and T. Fukami. “Structural Analysis of Molten NaNO₃ by Molecular Dynamics Simulation.” EPJ Web of Conferences 151 (2017): 01004.
J. Sun, H. Huang, H. Wu, Y. Lin, C. Yang, M. Ge, Y. Qian, X. Fu, and H. Liu. “HT-NMR Studies of the Be–F Coordination Structure in FNaBe and FLiBe Mixed Salts.” JACS Au 4, no. 6 (June 2024): 2211–2219.
S. Fayfar, R. Chahal, H. Williams, D. N. Gardner, G. Zheng, D. Sprouster, J. Neuefeind, D. Olds, A. Hwang, J. McFarlane, R. C. Gallagher, M. Asta, S. Lam, R. O. Scarlat, and B. Khaykovich. “Revealing the Complex Structure of Molten FLiBe (2LiF–BeF₂) by Experimental X-ray Scattering, Neutron Scattering, and Deep Neural Network-Based Molecular Dynamics.” (July 2023).
B. A. Frandsen, S. D. Nickerson, A. D. Clark, A. Solano, R. Baral, J. Williams, J. Neuefeind, and M. Memmott. “The Structure of Molten FLiNaK.” Journal of Nuclear Materials 537 (August 2020): 152219.
V. F. Grizzi, S.-C. Lee, and Y. Z. “First-Principles Investigation of the Effects of UF₄ and ThF₄ Fuels on the Structural, Dynamic, and Thermodynamic Properties of LiF–NaF.” The Journal of Physical Chemistry B 128, no. 23 (June 2024): 5676–5684.
A. R. Solano, A. Clark, K. P. Detrick, M. J. Memmott, and S. D. Nickerson. “Characterization of the Molten Salt FMgNaK through Ab Initio Molecular Dynamics and Experimental Density Measurements.” Journal of Nuclear Materials 557 (December 2021): 153248.
Golyshev, Vladimir D. “Experimental Investigation of the Thermal-Conductivity of Transparent Melts”, TVT, 21:5 (1983), 899–903; High Temperature, 21:5 (1983), 684–687,” 1983. https://www.mathnet.ru/php/archive.phtml?wshow=paper&jrnid=tvt&paperid=6160&option_lang=eng.
Golyshev, Vladimir D. “High-Temperature Thermophysical Properties of Nonscattering Semitransparent Materials I: Methods and Instrumentation for the Determination of Spectral Absorptivity and Thermal Conductivity of Melts,” no. 4 (1992): 367–77.
Khlebnikov, O. E., V. A. Sokolov, I. E. Veneraki, and A. N. Alabovsky. “Determination of Thermal Conductivity Coefficients of Lithium, Magnesium, Calcium, and Barium Fluorides in the Liquid State.” Thermophysical Properties of Substances 5 (1981): 97–101.
Harada, Makoto, Akihisa Shioi, Tsunetoshi Miura, and Shinsuke Okumi. “Thermal Conductivities of Molten Alkali Metal Halides.” Industrial & Engineering Chemistry Research 31, no. 10 (October 1, 1992): 2400–2407. https://doi.org/10.1021/ie00010a021.
Nagasaka, Y., and A. Nagashima. “Measurement of the Thermal Diffusivity of Molten KCl up to 1000°C by the Forced Rayleigh Scattering Method.” International Journal of Thermophysics 9, no. 6 (November 1, 1988): 923–31. https://doi.org/10.1007/BF01133260.
Gheribi, Aïmen E., Jesus A. Torres, and Patrice Chartrand. “Recommended Values for the Thermal Conductivity of Molten Salts between the Melting and Boiling Points.” Solar Energy Materials and Solar Cells 126 (July 1, 2014): 11–25. https://doi.org/10.1016/j.solmat.2014.03.028.
Khokhlov, V., I. Korzun, V. Dokutovich, and E. Filatov. “Heat Capacity and Thermal Conductivity of Molten Ternary Lithium, Sodium, Potassium, and Zirconium Fluorides Mixtures.” Journal of Nuclear Materials 410, no. 1 (March 1, 2011): 32–38. https://doi.org/10.1016/j.jnucmat.2010.12.306.
Merritt, Brian, Michael Seneca, Ben Wright, Noah Cahill, Noah Petersen, Austin Fleming, and Troy Munro. “Thermal Conductivity Characterization of Fluoride and Chloride Molten Salts Using a Modified Transient Hot-Wire Needle Probe.” International Journal of Thermophysics 43, no. 10 (August 10, 2022): 149. https://doi.org/10.1007/s10765-022-03073-2.
Nagasaka, Y., N. Nakazawa, and A. Nagashima. “Experimental Determination of the Thermal Diffusivity of Molten Alkali Halides by the Forced Rayleigh Scattering Method. I. Molten LiCl, NaCl, KCl, RbCl, and CsCl.” International Journal of Thermophysics 13, no. 4 (July 1, 1992): 555–74. https://doi.org/10.1007/BF00501941.
Robertson, Sean G., Ralph Wiser, Wonseok Yang, Dokyu Kang, Sungyeol Choi, Emilio Baglietto, and Michael P. Short. “The Curious Temperature Dependence of Fluoride Molten Salt Thermal Conductivity.” Journal of Applied Physics 131, no. 22 (June 8, 2022): 225102. https://doi.org/10.1063/5.0088059.
Rudenko, Alexey, Alexander Redkin, Evgeniya Il’ina, Svetlana Pershina, Peter Mushnikov, Yuriy Zaikov, Sergey Kumkov, Yalan Liu, and Weiqun Shi. “Thermal Conductivity of FLiNaK in a Molten State.” Materials 15, no. 16 (January 2022): 5603. https://doi.org/10.3390/ma15165603.
Smirnov, M. V., V. A. Khokhlov, and E. S. Filatov. “Thermal Conductivity of Molten Alkali Halides and Their Mixtures.” Electrochimica Acta 32, no. 7 (July 1, 1987): 1019–26. https://doi.org/10.1016/0013-4686(87)90027-2.
V. I. Fedorov, V. I. Machuev, “Thermal Conductivity of Fused Salts”, TVT, 8:4 (1970), 912–914; High Temperature, 8:4 (1970), 858–860. Accessed March 23, 2024. https://www.mathnet.ru/php/archive.phtml?wshow=paper&jrnid=tvt&paperid=7779&option_lang=eng.

## Slide 40: Additional Slides

## Slide 41: Previous Model Analysis
Models typically describe thermal conductivity in terms of a scale factor of energy storage, group velocity, and MFP of energy carriers
Model performance relative to measurements can help reveal physical mechanisms governing molten salt thermal conductivity
Gheribi Kinetic Theory, Cahill-Poll λmin (KTCPλ):
Zhao Phonon Gas Model (PGM):
Bridgeman-type:
Temp-varying modifier
Adjust to accounts for rotational, vibrational DOF
Normalized net flux in 1 of 3 dimensions
Adjusts MFP for valency

## Slide 42: Modeling Actinides
Gheribi - Kinetic Theory
KT methods build compositional dependency using a modifier to ideal conductivity, with a factor of mass fluctuation
KT performs well with ions of similar molar masses, but degrades with increasing disparity of molar mass, providing unrealistic estimations for actinides
MUF4 = 314 g/mol
MLiF = 25.9 g/mol
FLiBe+2%UF4
FLiBe
PGM underpredicts most λ, but approaches measured value with increased actinide presence. Why?
What we need:
More actinide data with compositional/temperature variation
Develop modeling ability for actinides
Reference 31

## Slide 43: Model Performance
Does the variation in model results sufficiently replicate measurement uncertainty?
KT uses fundamental mixing rules for property values (Cp, Vm, vsound)(cite Gallagher). These are applied to PGM for analysis.
Mm and vsound dominant influential parameters in both Gheribi and Zhao models; molten salt sound velocity values are subject to significant uncertainty.
Gheribi’s Cahill-Poll λmin provides best parameter sensitivity confinement
 | KTemp |  | KTCP | PGM
vsound,m | 15% |  |  | -2.1%
v’sound (slope) |  |  |  | 21%
Vm | -15% |  |  | -1.3%
V’ (slope) |  |  |  | 14%
Cp | 15% |  |  | 15%
%Deviation of estimated properties using mixing rules from measured values for eutectic FLiNaK
Comparison of FLiNaK model predictions using mixture values obtained via measurements or fundamental mixing rules.
See reference 10

## Slide 44: Review - Kinetic Theory
Generalized Energy Carriers
Kinetic theory model works for ideal gases because there exists only one type of energy carrier with measurable average attributes (number density, velocity, volumetric heat capacity).
For generalized energy carriers, the problem becomes how to characterize and measure energy carriers.
Unit volume in terms of average velocity
dx
dA
Unit area
Unit distance
Number density
Unit distance travelled in unit time 𝑑𝑡 at average velocity ⟨𝑣⟩
Number of energy carriers (particles, phonons, etc.) that will cross plane of unit area per unit time
+x
-x
1/6 will be moving towards surface
x
y
z
1/3 of particles will have motion in any given direction
x
y
z

## Slide 45: Review - Kinetic Theory
Generalized Energy Carriers
To define , we need to characterize the effective heat capacity, group velocity, and mean free path of the energy carriers.
x=0
Hot
Cold
x
y
z
x-λ
x+λ
Mean free path before collision (energy transfer)
Change in energy across unit plane per unit time—heat flux
Energy change proportional to definition of internal energy
Taylor series of about
Thermal conductivity in terms of energy carrier properties
Volumetric constant pressure specific heat capacity
Heat flux in terms temperature gradient

## Slide 46: Structural Coherence Length
Disruption Function
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
Most efficient separation distance for vibrational energy transfer.
Disruption factors :
: Non-ideal recipient probability factor
Chances of interacting with a like-charge ion instead of ideal oppositely charged ion (typically very small due to charge ordering).
Dependent only on the first peak, which is gives the probability distribution around any ion in the chain.
Accounts for the potential decoherence caused by non-deal recipient ions
Applied starting at second transfer

## Slide 47: Structural Coherence Length
Disruption Function
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
High ratio of peak height to first minima corresponds to very strong bond
Subsequent peaks are not determined by interaction potential with central ion—dictated by packing density
Non-zero first minima indicates relative affinity for diffusion
Disruption factors :
: Non-ideal recipient probability factor
: Bond strength factor
Ratio between 0 (bond allows no ions to escape) and 1 (no interaction between ions), related to diffusion coefficient[1].
This accounts for the potential inefficiency of energy transfer across a cation-anion pair
Applied starting at second transfer
[1] Hines, A.L., Walls, H.A., 1979. Determination of self diffusion coefficients using the radial distribution function. Metall Trans A 10, 1365–1370. https://doi.org/10.1007/BF02811992

## Slide 48: Structural Coherence Length
Disruption Function
Disruption factors :
: Non-ideal recipient probability factor
: Bond strength factor
: Phonon transfer factor
Ratio of encountering ion other than given ion pair.
This accounts for the potential inability of an ion chain to sustain a phonon—requires at least 3 ions
Applied starting at third transfer
Relative bond strength given by peak-minima ration, exponent simulating the Leonard-Jones potential attractive term
For
Assuming out-of-phase phonons cannot be sustained
Harmonic oscillator frequency function of bond strength and reduced mass
Reduced mass of cation-anion pair
Relative proportional frequency factor
Decoherence induced proportional to concentration of ion pair

## Slide 49: Structural Coherence Length
Disruption Function
Disruption factors :
: Non-ideal recipient probability factor
: Bond strength factor
: Phonon transfer factor
Ratio of encountering ion other than given ion pair.
This accounts for the potential inability of an ion chain to sustain a phonon—requires at least 3 ions
Applied starting at third transfer
Chart: LiF - PDF
| 1.877445579 | 4.3967871819999997 | 6.8563477969999997 | 9.7685358870000005
+- Peaks | 1.2421 | 0.45071 | 0.37613 | 0.34527 | 0 | 0
++ Peaks | 0.59536 | 0.39771 | 0.35861
Li-F | 0.017394 | 0.06754 | 0.11897 | 0.20255 | 0.30798 | 0.56579 | 0.85445 | 1.0897 | 1.226 | 1.2421 | 1.172 | 1.0499 | 0.92002 | 0.85445 | 0.7233 | 0.61015 | 0.51757 | 0.43785 | 0.37099 | 0.32213 | 0.22441 | 0.18326 | 0.16012 | 0.16012 | 0.23984 | 0.2707 | 0.2887 | 0.42242 | 0.45071 | 0.44299 | 0.43528 | 0.42499 | 0.40185 | 0.3607 | 0.31184 | 0.2887 | 0.28098 | 0.28098 | 0.37613 | 0.37613 | 0.35299 | 0.34527 | 0.33756 | 0.32984 | 0.32213 | 0.31184 | 0.31184 | 0.33756 | 0.34527 | 0.34527 | 0.34527 | 0.33756 | 0.33756 | 0.32984 | 0.32984 | 0.32213 | 0.32213 | 0.32213 | 0.32213 | 0.32213
Li-Li | 0.001566 | 0.00783 | 0.029738 | 0.057682 | 0.081684 | 0.11769 | 0.16269 | 0.22698 | 0.26779 | 0.29911 | 0.34609 | 0.40559 | 0.43691 | 0.46099 | 0.48778 | 0.52228 | 0.56032 | 0.59536 | 0.57436 | 0.54011 | 0.52143 | 0.4745 | 0.42499 | 0.39713 | 0.36658 | 0.33916 | 0.31037 | 0.28248 | 0.25526 | 0.23333 | 0.2443 | 0.26152 | 0.28355 | 0.32556 | 0.35446 | 0.38127 | 0.39771 | 0.39726 | 0.37069 | 0.34776 | 0.32241 | 0.30694 | 0.29597 | 0.29911 | 0.31642 | 0.34371 | 0.35705 | 0.35861 | 0.34452 | 0.33356 | 0.32573 | 0.31633 | 0.32103 | 0.32886 | 0.34139 | 0.34609 | 0.34452
+
+
-
+
+
-
Dissimilar ions cannot sustain minimum vibrational mode; transfer ends at first ion
Ion sequence of similar masses/bond strength can sustain coherent longitudinal wave

## Slide 50: Measurement Efforts
Developed thermal conductivity measurement device at BYU
Requires minimal sample size and test duration, enabling higher throughput for compositional studies
Building new version to measure actinide-bearing salts at higher temperature range (≤1100°C)
Modified Transient Needle Probe
Chart: Time (s)
Chart: Temperature (C)
| 320.16072325464501 | 330.10547463586101 | 340.050226017076 | 350.17579105976802 | 360.12054244098402 | 370.06529382219901 | 380.01004520341502
 | 0.54492 | 0.55086 | 0.58498 | 0.57042 | 0.56121 | 0.53783 | 0.54454

## Slide 51: Needle Probe
Solves multi-layer heat diffusion equation for λ and cp (and ρ if needed) to fit the analytical model to the temperature profile
Can select time frame for the fitting process according to regime most influenced by sample properties (from COMSOL sensitivity analysis)
Thermal quadrupoles to solve heat diffusion equations
Transform to Laplace space for solvable algebra
Solve for Laplace heat rate with Bessel functions
Adapt for layers system of equations
Numerically solve for sample properties to fit the analytical temperature to the temperature profile
λsample, cp,sample, ρsample